## Slide 1
5th September 2018
X-ray CT and IBFEM to inform the additive manufacture process
EBM of Ti-6Al-4V
S Tammas-Williams
F Derguti, F Leonard, PB Prangnell, I Todd, PJ Withers, H Zhao

## Slide 2: Fatigue crack initiation mainly from pores

## Slide 3: Correlate morphologies

## Slide 4: Correlate to manufacturing

## Slide 5: Correlate to manufacturing

## Slide 6: Correlate to strategy

## Slide 7: Can we get rid of them post AM?
HIPed
As-built

## Slide 8: However…
Most pores are caused by argon bubbles

## Slide 9: Pores reopen

## Slide 10: Correlate sizes

## Slide 11: Only gas pores reopen

## Slide 12: Life against defect size

## Slide 13: Life against defect size
√A = 105.1(±0.2) · Nf -0.67(±0.04) R2 = 0.99

## Slide 14: Why this pore?
5 mm
There are hundreds!

## Slide 15: Are all pores created equal?

## Slide 16: Are all pores created equal?
Simple empirical relationship based on idealised FEM

## Slide 17: Crack initiation

## Slide 18: Crack initiation can be predicted

## Slide 19: Crack growth imaged by CT
Increasing number of cycles

## Slide 20: Crack growth imaged by CT

## Slide 21: Influence of Pores on Crack Growth Rate
103k Cycles
104k Cycles

## Slide 22: Influence of Pores on Crack Growth Rate
δ < 0.3 %

## Slide 23: Can we optimise manufacturing based on what we have learnt?
√A = 105.1(±0.2) · Nf -0.67(±0.04) R2 = 0.99
Nf | √An (µm)
10,000 | 240
20,000 | 150
40,000 | 90
80,000 | 60
160,000 | 40

## Slide 24: Samples were machined from “bulk” material

## Slide 25: Effect of melt strategy on defect population
S. Tammas-Williams, I. Todd, et al., XCT Analysis of the Influence of Melt Strategies on Defect Population in Ti-6Al-4V Components Manufactured by Selective Electron Beam Melting, Mater. Charact. 102 (2015) 47–61. doi:10.1016/j.matchar.2015.02.008.

## Slide 26: Effect of melt strategy on defect population

## Slide 27: Correlate machining depths to life
P = 1 – e-λ

## Slide 28: Modify melt + machining strategy
P = 1 – e-λ

## Slide 29: Summary and references
S. Tammas-Williams et al., Influence of Porosity on Fatigue Crack Initiation in Additively Manufactured Titanium Components, Sci. Rep. 7 (2017) 7308. doi:10.1038/s41598-017-06504-5
S. Tammas-Williams et al., XCT Analysis of the Influence of Melt Strategies on Defect Population in Ti-6Al-4V Components Manufactured by Selective Electron Beam Melting, Mater. Charact. 102 (2015) 47–61. doi:10.1016/j.matchar.2015.02.008.
S. Tammas-Williams, P.J. Withers, I. Todd, P.B. Prangnell, Porosity regrowth during heat treatment of hot isostatically pressed additively manufactured titanium components, Scr. Mater. 122 (2016) 72–76. doi:10.1016/j.scriptamat.2016.05.002.
S. Tammas-Williams, P.J. Withers, I. Todd, P.B. Prangnell, The Effectiveness of Hot Isostatic Pressing for Closing Porosity in Titanium Parts Manufactured by Selective Electron Beam Melting, Metall. Mater. Trans. A. 47 (2016) 1939–1946. doi:10.1007/s11661-016-3429-3.